Technical data sheet:

Mohawk Via Laid: expressive colour and texture

Mohawk Via Laid combines a soft texture and with a crisp laid pattern applied to the paper during the papermaking process. The versatile laid surface helps deliver your message with a subtle, tactile twist.

Via Laid is available exclusively through Europapier in white and natural shades in writing, text and cover weight and with matching envelopes.

- Specified by the US print and creative communities for over 25 years

- Delivering Mohawk quality and performance at a budget-friendly price point

- Excellent on-press performance – uniform, stable and consistent

- Natural shade produced with 30% PCW

- Manufactured with wind energy

- FSC certified

| FINISH | SHADE | GSM | CALIPER [µ] | OPACITY | TAPPI | CIE | PPI |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Laid | Pure White | 100 | 147 | 94 | 96 | 143 | 314 |
|  |  | 120 | 181 | 94 | 96 | 143 | 281 |
|  |  | 220 | 343 | 98 | 96 | 143 | 156 |
|  |  | 270 | 381 | 99 | 96 | 143 | 133 |
|  |  | 350 | 533 | 99 | 96 | 143 | 95 |
|  | Natural | 100 | 147 | 93 |  |  | 314 |
|  |  | 120 | 181 | 94 |  |  | 281 |
|  |  | 220 | 343 | 98 |  |  | 156 |
|  |  | 270 | 381 | 99 |  |  | 133 |
|  |  | 350 | 533 | 99 |  |  | 95 |